Aluminium Spray

DESCRIPTION

Loctite 7801 spray dries to form a permanent corrosion protective coating at room temperature on all metal surfaces  The excellent appearance of this coating makes it suitable for finishing operations.

APPLICATION

This product may be used to touch up metal parts after welding or machining operations, e.g. repair to crash barriers, railings or other metalwork.

DIRECTIONS FOR USE

Shake well before use

Spray on to clean parts, where possible, from a distance of 20 - 30cm to give a uniform film.

PRODUCT PROPERTIES

| Base | Aluminium filled resin |
| --- | --- |
| Colour | Grey |
| Odour | Light |

Density @ 20ºC, g/ml

NFT 60 101/ISO 3675/DIN 51 757

0.8

Viscosity @ 20ºC, mm²/s

NFT 60 100/ISO 3104.3105

DIN 51 562

10

Flash point, ºC

| NFT 60 118/DIN ISO 2592 | Not Applicable |
| --- | --- |
| Tackfree time (Dry to touch), seconds | 20 |

Cure time, hours

for handling strength

for functional strength

1

24

AEROSOL CHARACTERISTICS

Propellant,

Weight, %

CO2

| 3 |
| --- |
| PERFORMANCE |
|  | Salt Spray Test (5%, 35ºC) NFX 41002 (Ri NFT 30 071/ISO 4628) |

0  -  24hr	Ri 0

24  -  48hr	Ri 1

48  -  72hr	Ri 2

72  -  96hr	Ri 3

96  - 120hr	Ri 4

after 120hr Ri 5

Recommended Operating Temperature Range, ºC

-45 to +550