|  | Food Approved Silicone Grease (Смазка силиконовая для оборудования пищевой промышленности) 26559 |
| --- | --- |

DESCRIPTION

Loctite 8104 is a silicone valve and packing grease suitable for use on equipment in the food processing industry It may also be used on bearings at low speeds.

APPLICATION

Suitable for lubricating plastic and elastomeric components, e.g. valves and joints in hot and cold water systems.  May be used to assist fitting of "o" rings.

APPROVALS

Approved for incidental food contact according to:

- FDA-21-CFR-178.3570

(USDA H1 Registration)

- CNERNA Guide 1992 (France).

DIRECTIONS FOR USE

Apply to clean parts where possible, as conventional grease, by means of brush, spatula or grease gun.  May be used in automatic lubrication systems.  Loctite cleaners 7063 or 7070 may used to remove grease residues from nipples and lubricated parts..

Follow manufacturer's recommendation for lubrication of bearings (quantity, frequency, etc.).

Avoid excessive greasing.  Other grease residues may not be compatible with Loctite 8104.

Do not apply to conveyors while food is being transported

PRODUCT PROPERTIES

| Base | Silicone oil/Silica gel |
| --- | --- |
| Colour | Colourless |
| Odour | Odourless |
| Density at 20ºC g/ml NFT 30 020/ISO 2811/ DIN 51 757 | 1.0 |
| Consistency NGLI Class NFT 60 162/DIN 51 818 | 2/3 |
| Worked Penetration ( 0.1mm) @ 25ºC and 60 strokes NFT 60 132/DIN/ISO 2137/IP50 | 220/250 |
| Drop Point, ºC NFT 60 102/DIN/ISO 2176/ IP132 Spirit content, % | None 10 |
| PERFORMANCE |  |
| Hoffman Oxidation (100hr) ASTM D942, psi | <5 |
| Corrosion on Copper 3 hours @ 100ºC ASTM D4048/NFM 07 015/ ISO 2160/IP112 | 1a |
| Loading Test-4 ball IP239/NFE 48 617/ DIN 51 350-5/ASTM D2596 | Not Recommended for Silicones |
| EMCOR Test, NFT 60 135/DIN 51 802/ IP 220 | 1 |
| Recommended Operating Temperature Range, ºC | -50 to +200ºC |
| DN Factor (Ndm), max. | 50,000 |